## Slide 1: GEM R&D at USTC
Wenhao You
Department of Modern Physics, University of Science and Technology of China
State Key Laboratory of Particle Detection and Electronics, USTC-IHEP, China
2017-07-27
9th Workshop on Hadron physics in china and Opportunities Worldwide, Nanjing University

## Slide 2
Introduction
Progress of the 1m × 0.5m GEM
APV25 readout system and the spatial resolution of the 30cm×30cm GEM
Conclusion and future work
Outline

## Slide 3
GEM foil structure:
Cu: 5 µm
Kapton: 50 µm
Diameter: 60 µm
80 µm
Pitch: 140 µm
GEM detector
Characteristics:
Position resolution ~100um
High rate capability
Excellent radiation hardness
Flexibility in shape and design
80um
60um
140um

## Slide 4
Assembly techniques for large-size GEM
Advantages：
1. assembling process is easy and fast
2. no dead area inside the active area
3. uniform gas flow
4. detachable
We choose the self-stretching technique, and have gained many experience through the 30cm×30cm GEM detectors.
Gluing technique
Self-stretching technique (from CERN)
stretching
Gluing inner spacer
Readout PCB

## Slide 5
1m×0.5m GEM detector
Copper X-ray
1m×0.5m GEM
Pre-Amp
Shaper
HV
MCA
The active area is divided into 200 sectors (5cmX5cm)
Triple-GEM
1m×0.5m
3mm-2mm-2mm-2mm
Structure
Testing system

## Slide 6
Relative Gain：mean~0.44
sigma~0.19
variation~43%
Energy resolution：mean~0.23
sigma~0.023
variation~10%
Gain uniformity still has room for improvement.
Uniformity result
Variation= σ/Mean
Energy resolution= FWHM/Peak

## Slide 7
The stretching screws will be blocked by the outside frame when it moves with the inner frame, and the tilted screws cause the gas leakage.
Problems of our original self-stretching design
folds
Screw and O-ring
Tension is non-uniform and small after stretching GEM foils
These problems will finally influence the performance of the detector.

## Slide 8
Simulation condition:
1m×0.5m GEM;
Structure ： 3mm-2mm-2mm-2mm；
Working voltage: 4kV.
Tension simulation and test
Testing result:
Overall foil extension is about 2.5mm at 500N/m.
Maximum deformation ~100um at 500N/m, acceptable
tension(N/m)
sag(um)
Deformation at different place on single foil
Tension sensor

## Slide 9
An improved GEM stretching method
Sliding self-stretching technique
Using this technique, a large-size GEM prototype (1m×0.5m) has been successfully built, and we’ve tested it.
nut
Inner frame
Stretching screw
GEM foils can move freely up to 5mm with respect to the main frame

## Slide 10
Energy resolution is as well, the relative gain uniformity is much better;
The sliding self-stretching technique improves the performance of the GEM significantly.
Test result of 1m×0.5m GEM with new technique
New technique relative Gain：
mean~0.73
sigma~0.12
variation~16%
Original technique relative Gain：
mean~0.44
sigma~0.19
variation~43%

## Slide 11
GEM readout system based on APV25
Position resolution testing system
Drift foil
Double-GEM
Pitch: 400um;
Strip width:
x(80um),
y(350um)
Readout PCB
50 um slit

## Slide 12
Effective gain ~3199, 400V for each GEM foil；
Input charge: ~19 fC，linearity of APV25 is well.
Gain and spark probability test
Gain uniformity test
Average = -4.04nA
Sigma = -0.031nA
Variation= σ/Mean
Spark probability test
Time: 6 hours;
Spark probability: 8.95E+7 signal per spark.

## Slide 13
Spatial resolution result
Typical spatial resolution： x~65um; y~70um
σ=63um
σ=68um
Frog bone
2-D imaging

## Slide 14
Future plan for low mass GEM
Standard GEM foil
Copper-free GEM foil
Copper Free Area
Light Material(Rohacell)
Copper-free
No inner screw
Metal screw
Thanks for R. De Oliveira’s help on Copper-free GEM
Double-sided adhesive
No metal screw

## Slide 15
System setup:
System platform;
Four 40cm×40cm GEM;
Two 15cm×15cm scintillator;
Two PMT;
readout system based on APV25.
Future plan for cosmic ray system
15cm×15cm scintillator
10cm×10cm GEM
System platform
As the first step, we tried to use the 10cm×10cm to setup the cosmic ray system, then the larger GEM.

## Slide 16
We developed a new sliding self-stretching technique to assemble GEM detectors;
This new stretching technique improved the gain uniformity of 1m×0.5m GEM from 43% to 16%;
Typical spatial resolution of the 30cm×30cm double-GEM is about 65um(x-direction) and 70um(y-direction);
Spatial resolution of the 1m×0.5m GEM with the APV25 readout system will be tested;
We will work on the low mass GEM research;
We will finish the setup of the cosmic ray system.
Conclusion and future work
Thanks